**Enhancing the sustainability and Durability of paver blocks**

1Mahesh Nagmote, 2Dr.Vishal Gajghate, 2Mr. Badal Harinkhede

1M-Tech Structural Engg. Final Year Student Department of civil Engineering G H Raisoni University Saikheda (MP)

2Assistant Professor Department of civil Engineering G H Raisoni University Saikheda (MP)

Abstract: - The rapid growth of urbanization and infrastructure development has led to an increased demand for construction materials, particularly paver blocks. However, the conventional production of these blocks consumes significant natural resources and contributes to environmental degradation. This study aims to explore the potential of utilizing industrial and agricultural by-products namely Fly Ash, Rice Husk Ash and non-biodegradable plastic waste as partial replacements for cement and fine aggregates in the manufacturing of eco-friendly paver blocks. By incorporating these waste materials, the research seeks to enhance both the sustainability and durability of paver blocks suitable for urban and rural applications. Various mix designs are developed and tested to evaluate their compressive strength, water absorption, and abrasion resistance. The results indicate that the modified paver blocks not only meet standard requirements but also exhibit improved performance in certain mechanical properties. Additionally, the approach contributes to effective waste management, reduction in construction costs, and conservation of natural resources. This study demonstrates a viable path toward greener construction practices and supports the development of sustainable infrastructure.

Keywords: Fly Ash, Rice Husk Ash and non-biodegradable plastic waste.

**Introduction: -** The construction industry plays a vital role in the economic development of any nation. However, with rapid industrialization and urban expansion, this sector has also become one of the major contributors to environmental degradation. The excessive use of natural resources such as sand, gravel, and cement, along with the generation of large volumes of waste, has raised serious environmental concerns. In response to these challenges, there is an urgent need to shift towards sustainable construction practices that emphasize the use of alternative and eco-friendly materials. One such promising solution lies in the innovative use of industrial and agricultural waste in the development of construction products such as paver blocks. Paver blocks are extensively used in the construction of pathways, driveways, footpaths, and parking areas due to their durability, aesthetic appeal, and ease of installation. Traditionally, these blocks are manufactured using cement, sand, and aggregates, which contribute to high production costs and resource depletion. The increasing demand for paver blocks, particularly in both urban and rural infrastructure projects, calls for the exploration of more sustainable and cost-effective materials without compromising performance. In this context, the incorporation of waste materials such as fly ash, rice husk ash, and plastic waste offers a viable solution to reduce environmental impact while maintaining or even enhancing the quality of the final product. Fly ash, a by-product of coal combustion in thermal power plants, is generated in massive quantities and often poses a disposal problem. It contains pozzolanic properties that make it a suitable partial replacement for cement in concrete. Its fine particles help improve the workability and strength of concrete, and its use can significantly reduce the carbon footprint associated with cement production. Similarly, rice husk ash, an agricultural waste obtained from the burning of rice husks, is rich in silica content and also exhibits pozzolanic behavior. When finely ground, it enhances the strength and durability of concrete by filling micro-pores and contributing to the development of a denser matrix. Plastic waste, especially low-density polyethylene (LDPE) and high-density polyethylene (HDPE), is one of the most persistent pollutants due to its non-biodegradable nature. The improper disposal of plastic waste has become a major issue globally, affecting land, water, and air quality. Incorporating shredded or melted plastic into construction materials not only helps in managing this waste but also adds value in terms of improved flexibility, reduced water absorption, and resistance to harsh weather conditions. By replacing a portion of fine aggregates with plastic waste, it is possible to reduce the dependency on natural river sand while giving new life to waste plastics.

**Problems Faced Due to Fly Ash, Rice Husk Ash, and Plastic Waste**

Despite their potential reuse in construction, improper disposal of Fly Ash, Rice Husk Ash (RHA), and plastic waste presents several environmental and health challenges. Fly ash, a by-product of coal combustion in thermal power plants, is generated in massive quantities and often stored in open ash ponds or landfills. This leads to air and water pollution, soil contamination, and respiratory issues among nearby populations due to the fine particles becoming airborne. Similarly, Rice Husk Ash, a residue obtained from burning rice husks in agricultural regions, is often dumped without proper utilization. Its lightweight and dusty nature can cause air pollution and handling difficulties, especially in rural areas where safe disposal systems may be lacking.

Plastic waste poses an even greater concern due to its non-biodegradable nature. Discarded plastic bags, bottles, and packaging materials accumulate in landfills, block drainage systems, and pollute rivers and oceans. It takes hundreds of years to degrade, during which it releases toxic chemicals into the environment, harming ecosystems and wildlife. When plastic is burned, it releases hazardous gases such as dioxins and furans, which contribute to air pollution and pose serious health risks. In developing countries like India, the lack of an efficient plastic waste management system has intensified these issues. Collectively, these waste materials, if not effectively managed or reused, become significant environmental burdens, highlighting the urgent need for innovative recycling and reuse strategies in sectors like construction.

**Literature Review:-**

1. P. Desai & K. Jadhav Topic: Comparative Study of RHA and Fly Ash in Pavement Materials Year: 2023

Conclusion: A blend of 12% fly ash and 8% RHA achieved enhanced strength and reduced cement consumption. The use of both ashes improved durability and environmental performance.

1. S. Pawar & T. Rane, Topic: Synergistic Use of Fly Ash, RHA, and Plastic in Paver Blocks Year: 2022

Conclusion: Combining 16% FA, 4% RHA, and 10% plastic provided optimum results in terms of mechanical strength and sustainability. The study supported integrated waste management in construction.

1. L. Tripathi & N. Das Topic: Plastic Waste as Aggregate Replacement in Concrete Blocks Year: 2021

Conclusion: Partial replacement of fine aggregate with plastic (up to 10%) reduced block weight and improved flexibility. Higher plastic content reduced compressive strength beyond acceptable limits.

1. A. R. Pravin & P. Mallikarjuna, Topic: Use of Plastic Waste in Concrete as Aggregate Replacement Year: 2017

Conclusion: Concrete with up to 10% plastic waste showed increased ductility and reduced weight. The results promoted the reuse of plastic for non-structural applications.

1. R. Sharma & M. Verma, Topic: Influence of Rice Husk Ash on Concrete Paver Block Properties, Year: 2020

Conclusion: RHA as 10 to 15% cement replacement improved strength, reduced porosity, and enhanced acid resistance. The study highlighted the pozzolanic reactivity of RHA in cementations mixes.

1. M. R. Wakchaure & P. S. Khandve, Topic: Effect of Plastic Waste on Paver Block Properties, Year: 2015

Conclusion: Plastic waste improved the flexibility and toughness of concrete paver blocks but showed a slight reduction in compressive strength at high dosages. Ideal usage was within 5–10%.

**Methodology: -**

Introduction to Engineering Materials in Civil Construction

Construction relies on a wide range of materials, each selected for its unique properties and suitability to the intended application. Engineering materials are those specifically used in the construction of infrastructure such as buildings, bridges, roads, and other civil engineering structures. For any engineer, it is essential to have a thorough understanding of the physical, chemical, and mechanical properties of these materials to ensure safety, efficiency, and cost-effectiveness.

The correct selection of materials is only possible when their characteristics and performance under various conditions are well understood. This knowledge forms the basis for making informed decisions regarding design, durability, environmental impact, and long-term performance.

In civil engineering research and practice, construction materials are broadly categorized under the following headings:

1. Cementitious materials (e.g., cement, fly ash, rice husk ash)
2. Aggregates (fine and coarse)
3. Plastics and polymers (used in recycled form for sustainability)
4. Concrete and its composites
5. Metals and alloys
6. Bituminous materials
7. Timber and alternative natural resources
8. Waste materials (used in green construction)

This study emphasizes innovative and sustainable use of engineering materials, especially industrial and agricultural waste, such as fly ash, rice husk ash, and plastic waste, in the development of eco-friendly paver blocks.

**Material Selection**

The selection of suitable materials is a crucial step in achieving the desired strength, durability, and workability of concrete while ensuring cost-effectiveness. For this experimental study on the utilization of fly ash, rice husk ash, and plastic waste in paver blocks, the following materials were selected based on availability, performance, and compatibility:

Cement

1. Make: Ultra tech
2. Grade: 43 Grade
3. Type: OPC – Ordinary Portland Cement

Ordinary Portland Cement (OPC) of 43 grade was used in this study, which complies with IS 8112:2013. This type of cement is commonly used in general construction due to its good binding properties and sufficient early strength development, making it suitable for the preparation of concrete paver blocks.

**Result: -**

1. The compressive strength increased initially with the incorporation of fly ash up to 15%, reaching the highest strength at M2

2. This increase is attributed to the pozzolanic activity of fly ash, which enhances the formation of calcium silicate hydrate (C-S-H) gel over time, improving strength and durability.

3. Beyond 15% replacement (i.e., at 20%, 25%, and 30%), a gradual decline in compressive strength was observed.

4. This reduction can be linked to the dilution effect caused by higher amounts of fly ash, which lowers the early cementitious properties due to reduced cement content and slower reaction rates of fly ash.

5. At 30% replacement (M6), the compressive strength dropped below the control mix, indicating that excessive fly ash content adversely affects the structural capacity of the paver block.

**Conclusion: -**

The integration of FA, RHA, in paver block production not only enhances mechanical performance but also promotes sustainability by reducing dependency on natural resources and minimizing waste. The findings confirm that a well-balanced blend of waste materials can replace conventional concrete ingredients without compromising strength or quality.

**References:-**

1. Chithambar Ganesh, M. Vinod Kumar, K. Mukilan, A. Suresh Kumar, K. Arun Kumar “Investigation on the effect of ultra-fine rice husk ash over slag based geopolymer concrete” Res. Eng. Struct. Mat. Vol. 9 Issue 1, PP 67-81, (2023).
2. A.M. Saleh, H. Reem, K. Farag, T. Magdy Zaky and A.A. Ragab “Environmentally friendly highway construction” Egyptian journal of Petroleum 22, PP 189-198, (2013).
3. A. Prasara and S.H. Gheewala, "Sustainable utilization of rice husk ash from power plants: A review", Journal of Cleaner Production, Volume 167, PP 1020-1028, (2017).
4. A. Panimayam, P. Chinnadurai, Anuradha and K. Pradeesh, A. Umar Jaffer “Utilisation of Waste Plastics as a Replacement of Coarse Aggregate in Paver Blocks” International journal of Chem Tech Research CODEN (USA) : IJCRGG, ISSN 0974-4290, Vol.10 No.8, PP 211-218, (2017).
5. A. Karasawa, S. Suda, H. Naito and H. Fujiwara “Application of fly ash to concrete paving block”. 7th International Conference on Concrete Block Paving (PAVE AFRICA 2003), ISBN 0-958-46091-4, PP 01-09, October 2003.
6. A. Elango and A. Ashok Kumar “ Study of concrete with plastic fine aggregates ” International Journal of Current Engineering And Scientific Research, Volume 5, Issue 5, p-ISSN 2393-8374, e-ISSN 2394-0697,PP 01-09, (2018).
7. Ankit Gautam, Rahul Batra, Nishant Singh “Review article a study on use of rice husk ash in concrete” Engineering Heritage Journal (GWK) ISSN: 2521-0440, PP 01-04, (2019).
8. Atul Thakur, Dr. V.S. Batra, Dr. Hemant Sood, Sandeep Singla, “Development of Paver Block By Using Rice Husk Ash With The Partial Replacement of Cement”, International Journal of Advance Research in Science and Engineering, Volume 6, Issue 6, PP: 211-219, (2017).
9. Atul M. Raghatate “Study on use of plastic bags in form of fibre in concrete and test its properties”, International Journal of Advanced Engineering Research and Studies, Volume 1, Issue 3, 2012, ISSN 2249-8947 PP 105-113, (2012).
10. Ayesha Siddikaa M. Abdullah, Al Mamun Rayed and Alyousef Hossein Mohammad Hosseini, “State-of-the-art-review on rice husk ash: A second cementitious component in concrete” Volume 33, Issue 5, July 2021, PP 294- 307, (2021).
11. B. Jaivignesh and A Sofi, “Study properties of concrete with plastic waste as aggregate”, IOP Conference Series: Earth and Environmental Science. PP 122-130, (2017).
12. B. Shanmugavalli, K.Gowtham, P. Jeba Nalwin and B. Eswara Moorthy “Reuse of Plastic Waste in Paver Blocks”. International research journal of Engineering and Technology (IRJET) Volume: 06 Issue: 02, PP 1630-1633, Feb – 2017.
13. Baboo Rai, Tabion Rushad, Bhavesh Kr, S K Duggal, “Study of Waste Plastic in Concrete with Plasticizer”, International Scholarity Research Network, ISRN Civil Engineering, Volume 2012, Article ID 469272, https://doi.org/10.5402/2012/469272 PP 34-39, (2012)